## Slide 1
Name: Yun-Chen Tsai
Advisor: Prof. Yu-Jung (Yuri) Lu1,2
1Research Center for Applied Sciences, Academia Sinica, Taipei 11529, Taiwan
2Department of Physics, National Taiwan University, Taipei 10617, Taiwan
Date: 2024.xx.xx

## Slide 3: Key findings
At low VDS, conduction is ohmic; at higher VDS, it becomes SCLC
The current follows I ∝ Vm, with m ≈ 2 at room T, increasing as temperature decreases, consistent with exponential trap distribution
A temperature-independent critical voltage Vc is observed, where I–V curves at different T intersect.
From Vc, trap densities were quantified: Nt∼1.5 – 2.3×1017 cm−3
Increasing gate voltage lowers Vc, showing that gate-induced carriers pre-fill traps.
The trap states likely originate from bulk MoS₂ disorder (sulfur vacancies, oxidation, structural inhomogeneity) rather than just substrate effects.

## Slide 4: Figure 1
Inset: SEM image
I–V curves at room T for different VBG
Linear and symmetric at low VDS,
showing quasi-ohmic contacts
I–V curves at VBG = 0 V across different T
Nonlinearity increases as T decreases, excluding Schottky/tunneling effects.
Work function:
MoS2: 5.1 eV
Au: 4.5 eV
(nonlinearity arises from SCLC)

## Slide 5
channel length ~80–200 nm

## Slide 6: Figure 2
Log–log I–V curves (room T, VBG=0).
At low VDS slope = 1 (ohmic)
At higher VDS slope → 2 (SCLC).
Temperature dependence:
slope increases from
1.7 (285 K) → 2 (205 K) → 3 (105 K)
Extrapolation of I–V curves at low T yields a T-independent critical voltage ≈4.3 V, giving trap density 2.3×1017 cm−3
Confirms exponential trap distribution and provides a method to quantify trap density
Dev 5
At RT > Tc, m = 1.7 < 2
At Tc, m = 2
At T < Tc, m increases

## Slide 7: Figure 3
I–V curves at VBG = 0, 20, 40 V for multiple T.
Intersection points (critical voltage) decrease with gate bias
High gate voltage fills more traps at equilibrium
reducing effective trap density and lowering Vc​

## Slide 9: ACKNOWLEDGEMENT
Lu Lab 2024